Zeolite Reactor setup.

1. Lift plunger, so remove the inner sleeve chamber.

2. Loosen top plate (Only on the 150 & 200) and move to just below lid.

3. Add media to a maximum of the height of the inner sleeve.

4. Secure top plate (Only on the 150 & 200) to the top of the inner sleeve using the two securing screws.

5. Place the inner sleeve chamber back into body of the reactor.

6. Postion the zeolite reactor in desired situation, sump etc and add pump to inlet of reactor.

7. Start pump and check reactor over to make sureevrythings running correctly.

8. Follow running instructions.

Note:

Extra media can be added above the inner sleeve, but this may cause friction between the media and chamber.

Running the Reactor.

To clean the material, push and pull the rod appr. 15-20 times. Keep the pump running during the cleaning process. Simple, fast and easy removal of mulm and deposits from the Zeolite (takes just a minute). It is important to clean the Zeolite daily.

For an enhanced nitrate and phosphate removal you can run the Zeolite in the reactor in an alternating environment of aerobic and anaerobic conditions. The micro-organisms/bacteria will aspirate more nitrate and phosphate then. This can be achieved by switching the pump of the filter on and off at an interval of 3 hours (the material must not be exposed to air while pump is off).

The outcoming slimy mulm which is found to be a valuable kind of bacteria plankton that is absorbed by many corals which in turn leads to more intense coloration. Furthermore it improves the keeping of Goniopora, Alveopora, horn corals and Heliofungia without problems.